## Slide 4
Source: Xu et al. (2015), Nanoscale
Source: Ramakrishna et al. (2015), Filtering Media by Electrospinning
Prepolymer Solution
Electrospinning Setup
Source: Koenig et al. (2019), Biomaterials

## Slide 5
Source: Turnbull et al. (2005), British Journal of Anesthesia
Notes: https://reader.elsevier.com/reader/sd/pii/S0007091217356404?token=9EB2903B9E2B04596F6EB5550D71804C8B9CD085B1B3D994D74CC8A10A6C848307D5B2E459CF537863BC9B520BDB41F9

## Slide 6
Vp > 12 kV
TCD
Mechanical Extrusion
Stationary Collector
X
Y
Straight Jet Regime
Taylor Cone formation
Chaotic Jet Regime
Solution Electrospinning
Polymer solution
Evaporation
+
+
Mechanical Extrusion
Stationary Collector
Limited
Chaotic
Jet Regime
Polymer Melt
Cooling
+
+
Melt Electrospinning
TCD
Vp < 12 kV
Q
Q

## Slide 7
1 mm
Spinning Time = 1 min | SES – 1min
200 μm
200 μm
Spinning Time = 3 min | SES – 3min

## Slide 8
Solution ES – 1min

## Slide 9
Our own calculations and literature review, we find that rotary jet spinning (RJS) has the capacity to meet the demand of medium-scale production of N95 grade nano-fiber material and seems to be the one that would be most applicable in this scenario[1]. RJS can produce nanofibers about 50x faster than electrospinning and does not involve the danger of high voltage [2] and is very simple to set up.

## Slide 10
Source: Badrossamay et al. 2010, Nano Lett, 10, 2257-2261
Notes: The RJS system consisted of a polypropylene reservoir with a diameter of 12.5 mm and height of 25.4 mm (Figure S1). The reservoir had two sidewall orifices with diameter (D) of 340
μm and L: D ratio of 9, where L is the orifice length depicted in Figure 1b. The perforated reservoir was attached to the shaft of a brushless motor (model BND23 from Peromatic GmbH, Switzerland) and rotation speed was controlled by a circuit board. The circuit is equipped with a manual rotation speed control to change the rotation of the motor before or during RJS. The polymer solution was continuously fed to the reservoir via polyethylene tube connected to a 50 ml syringe placed in the cradle of syringe pump (KD Scientific, Holliston, MA). Rotation started immediately after filling the reservoir. The resulting fibers were collected on a stationary round collector. Collected fibers were removed and weighed after certain period of time to evaluate production rate. The production rate was 5-6 g/h which is ~10 times higher than the production rate of standard electrospinning. To study effect of orifice geometry on fiber geometry, another orifice with diameter of 650 μm and L: D ratio of 5 was built.
The production rate was 5-6 g/h which is ~10 times higher than the production rate of standard electrospinning

## Slide 11
Source: Golecki et al. 2014, Langmuir, 30, 13369-13374
Notes: The RJS system used to manufacture fibers is depicted in Figure 1a. The RJS consisted of a brushless DC servo motor (Maxon Motor Company, Fall River, MA) attached to a
custom-fabricated reservoir with a 343 μm sidewall orifice. Solutions (1 mL) were spun at angular speeds, Ω, up to 75 000 rpm and collected at the spinning midpoint to ensure sample uniformity.

## Slide 12
Notes: The hollow metal rotary cone was used as spinneret (Figure 1A). The bottom and top diameters, the height, and the thickness of the hollow cone were 30, 7, 40, and 2 mm, respectively. The
cone was fixed coaxially to the DC electromotor with a nylon column. At the top of the nylon column, there was a plastic wafer with a thickness of 0.5mm and a diameter of 40 mm. The nylon
column and the plastic wafer were used to avoid static electricity. The outer surface of the cone was mechanically polished. Pieces of copper wires were brushed up against the cone as electrical
contacts.

## Slide 13
x
1 machine / Fab Lab
2,000 Fab Labs
600 g/hr
1,200,000 g/hr
=
or
706,000 masks / hr
< 600 g/hr
353
masks/hr
=
or
8,500 masks/day
/
1.7 gr filter material/mask
Source: Prakash Lab

## Slide 14
0.2 g/min
+ high yield (10s of g/hr)
+ simple setup
control over porosity
post - electrostatic charging for increasing filtration efficiency
Post proc for surface to volume ratio
100s of g/hr
ROTARY JET SPINNING
ELECTROSPINNING CONFIGS
FAB
SPINNER

## Slide 15
Cone electrode
Sheet Metal
Aluminum
Thickness = 2mm
40 mm
60 mm
Brushless DC Motor
30,000 RPM
Wood
10 mm
350 mm
Grounded Metal Grid